Indoor UPS and outdoor UPS Power System

Comprehensive Comparison Tables

| No. | Item | Indoor UPS | Outdoor UPS | Remark |
| --- | --- | --- | --- | --- |
| 1 | Set up Type | Group | Distributed | Erection of emergency systems should spread risk |
| 2 | Size | Big | Small | In the same capacity, C-LiFePO4 Lithium Batteries size, less than the Lead-acid battery 35% |
| 3 | Weight | Heavy | Lift | In the same capacity, C-LiFePO4 Lithium Batteries weight, less than the Lead-acid battery 50% |
| 4 | Dusty & Waterproof | IP44 or Non | IP67 |  |
| 5 | Power conversion efficiency | normal | better |  |
| 6 | Power supply mode | On-line/Interactive /Off-line | On-line | Online devices operate without disruption |
| 7 | Battery type | Lead-acid batteries | C-LiFePO4 Lithium Batteries | Lead-acid battery cannot cell management charging & discharge |
| 8 | Battery cycle life (for Indoor Used) | 300~450 times, Left 50-60% Power capacity | >2000 times | Outdoor UPS of C-LiFePO4 Lithium Batteries after 2000 times are still 80% power capacity |
| 9 | Service life (for Indoor Used) | 1.5 year | >7 year | Outdoor UPS of C-LiFePO4 Lithium Batteries for indoor used, will have more battery cycle life |
| 10 | Battery cycle life (for Outdoor Used) | 150~300 times, Left 50-60% Power capacity | >1100 times | Outdoor UPS of C-LiFePO4 Lithium Batteries after 1100 times are still 80% power capacity |
| 11 | Service life (for Outdoor Used) | 0.5~1 year (need replace 6 times in 3 years) | >3 year | Outdoor UPS of C-LiFePO4 Lithium Batteries real outdoor tested 3 years still 95%~ power capacity |
| 12 | Operation of high and low temperature | -0~45sheshidu | -20~70sheshidu | Lead-acid temperature 50 degrees operation easily damaged |
| 13 | RoHS | Does not meet the RoHS | accord with RoHS | 2015 Lead Acid disabled |
| 14 | Charging time | 8hrs | 1.5hrs | @95% Capacity, C-LiFePO4 Lithium Batteries can fast charge |
| 15 | High rate discharge | not allowed | Reliable | Outdoor UPS of C-LiFePO4 Lithium Batteries can supply 5~8 times current discharge |
| 16 | Memory effect | yes | no |  |
| 17 | Security | Releasing toxic gas and explosion hazards | No explosion risk | Outdoor UPS of C-LiFePO4 Lithium Batteries @short circuit conditions, maximum temperature up to 120~130°C, at the same time have the security design of the pressure relief valve, so no explosion risk |
| 18 | Maintenance costs | higher | lowest | Lead-acid batteries for use in outdoor environments, will face 6 times in 3 years replacement cost ; While operation due to frequent battery replacement issues, resulting in low system properly rate |
| 19 | System cost | Cheap | Expensive | Lead-acid as 1 price< deep Lead-acid as 3 times< Gen Lithium as 4~5 times < C-LiFePO4 Lithium as 6~7 times |
| 20 | System application | Indoor | Indoor and Outdoor | Outdoor UPS for indoor use, will have more Battery cycle life |